## Slide 1: Molecular Tailoring of Interfaces using Self-Assembled Monolayers: A Multi-scale Study of Roughness Effects
Session: Mechanics of Thin Films and Multi-Layer Materials
SES 2014, Purdue University, West Lafayette, IN
October 1-3, 2014
Philippe Geubelle, Professor
Aerospace Engineering
Amnaya P Awasthi, Post-doc
Aerospace Engineering
Nancy Sottos, Professor
Materials Science and Engineering
Martha E Grady, Graduate Student
Mechanical Engineering
University of Illinois at Urbana-Champaign, USA
Chen Zhang, Graduate Student
Aerospace Engineering

## Slide 2: Self-Assembled Monolayers
Ordered molecular assemblies formed spontaneously on surfaces by adsorption
Each unit comprises of the ‘head group’, ‘tail’ and ‘functional group’
Applications
  Wetting and adhesion
  Chemical resistance
  Nano-fabrication
  For studying membrane properties of cells
  Commercial application example: Rain-X
  Surface modifiers in MEMS and NEMS
  Bio-compatibility
  Thermal management of nano-electronics
  Nanoscale tailoring of interfaces
Scanning tunneling microscope image (15 nm x 15 nm) of a SAM of n-decanethiolate on Au{111} (Paul Weiss’ group, PSU)
SURFACE
MODIFIERS
INTERFACE
TAILORING
Terminal groups
Substrate
Thin film

## Slide 3: Molecular Mechanical Tailoring of Interfaces
In the literature…
  Experiments: Impact of SAM on adhesion using quasi-static techniques (super-layer tests, DCB, …)
    Example: Zhuk, Evans, Hutchinson and Whiteside, J. Mater. Research (1998): impact of COOH/CH3 functional groups on interface strength of epoxy film on Au/Ti/Si substrate
  Review article: Goertz and Moore, Prog. Surf. Science (2010)
  Modeling: Emphasis on constitutive properties of SAM
    Example: Wang, Liechti, et al., J. App. Mech. (2006): Hybrid continuum-molecular analysis of constitutive response of OTS on Si/SiO2
Objective: Investigate dynamic failure response of SAM using a combined experimental and modeling study
  Atomistic modeling of ‘SAM-enhanced’ interfaces
  Laser-based spallation experiments
  Continuum (cohesive) modeling of effect of roughness
Losego et al., Nature Materials, 2012

## Slide 4: Materials
Self-assembling molecules (Gelest Inc.)
Chemical | Formula | Shorthand Name
Dodecyltriethoxysilane | CH3(CH2)11Si(OC2H5)3 | DTES
11-mercapto-undecyltrimethoxysilane | SH(CH2)11Si(OC2H5)3 | MUTMS
11-bromo-trimethoxysilane | Br(CH2)11Si(OC2H5)3 | BrUTMS
11-amino-trimethoxysilane | NH2(CH2)11Si(OC2H5)3 | ATES
NH2
Br
SH
CH3
Mixed Monolayers
50% mole percent in solution
SiO2 Substrate
Notes: Also describe mixed monolayers here as well

## Slide 5: MD Model of DTES and MUTMS SAMs
SAM/Gold model built using Materials Studio
In-plane periodic unit cell of size 25A x 25A x 40A (Contains about 1500 atoms)
Captures SAM tilt with respect to Silica layer
Dodecyltriethoxysilane | CH3(CH2)11Si(OC2H5)3 | DTES
11-mercapto-undecyltrimethoxysilane | SH(CH2)11Si(OC2H5)3 | MUTMS
Velocity imposed on gold layer
Thermal equilibrium (at 300K) and spallation simulations performed using LAMMPS
MD analysis based on ReaxFF potential to model bond failure (Jarvi et al., J. Phys. Chem. A, 2011)
“Smooth” application of constant velocity along top Au atomic layers

## Slide 6: MD Predicted Cohesive Laws for DTES, MUTMS
T=300K, V0=30m/s,
strain rate = 4x1010 s-1
DTES
MUTMS
Work of separation ~ 0.3 J/m2
Interfacial strength ~ 0.75 GPa
Work of separation ~ 0.6 J/m2
Interfacial strength ~ 3 GPa

## Slide 7: SAM Functionalization Procedure
Piranha Solution
Clean
SAM bath
24 hours
SAM molecule, amine catalyst, toluene
Rinse Toluene, Ethanol,
DI water,
blown dry
Ellipsometry
Transfer Printing
Material Characterization
X-ray Photoelectron Spectroscopy (XPS)
Atomic Force Microscopy (AFM)
SAM layer thickness ~ 1 nm
Surface topography, surface roughness
Chemical information
“Soft” lithography process
Technique
Information Acquired

## Slide 8: Transfer Printing Method
Use PDMS stamp to peel off gold
Transfer Print to New Substrate
Peel off PDMS
SiO2/SAM/Au
2
1
3
4
Deposit Au on donor substrate
Losego et al. Nat. Mater. 11 (2012)

## Slide 9: Interfacial Strength Measurement
Transfer printed Au films (150 nm)
Fused silica / Si substrates (1.5 mm thick)
Nd:YAG spot size of 2.0 mm
Test over a range of fluences
Determine film failure optically
Specimen Schematic
Laser Spallation Technique

## Slide 10: Laser Spallation Setup
Grady et al. Thin Solid Films (2013)
sample holder
Nd:YAG focusing lens
beam splitting cube
photodiode detector
Nd:YAG filter
film
specimen
mirror
to
oscillo-scope

## Slide 11: Interferometric Data Analysis
Output Voltage Signal
Time (ns)
Voltage (mV)
Displacement
Time (ns)
Dispalcement (μm)
Substrate Stress Pulse
Time (ns)
Substrate Stress (GPa)
Interface Stress
Results from 1D Finite Element Model
Time (ns)
Interface Stress (MPa)
Notes: Lev and Argon studied geometric attenuation….negligible, minimal losses for 3-4 times radius of spot.
Barker 1972 experimental mechanics laser interferometry in shockwave research
Elastic wave equation slide 74, Junlan has nice derivation in JMPS paper

## Slide 12: Observed Film Failure
all scale bars are 500 μm
Increasing
Interfacial Strength
-NH2
-Br
-SH
-CH3
Notes: Transition into mixed monolayers

## Slide 13: Interfacial Strength Statistics
Interface strength determined at interface stress that initiates film failure in >85% tests
Measured interfacial strength much lower than MD predictions
Experimental | Numerical
25 MPa | 0.75 GPa
85 MPa | 3 GPa
DTES
MUTMS
DTES
MUTMS

## Slide 14: “Side Note”: Heat Transport Properties
Thermal conductance G=Q/ΔT measured using time-domain thermo-reflectance
SAM between quartz and gold film
Strong correlation between G and bond strength
Losego et al. Nature Materials. 2012.
Notes: TDTR is a modulated optical pump-probe technique that uses a pulsed Ti:sapphire laser to monitor temperature decay by thermoreflectance with picosecond resolution.

## Slide 15: Interface Strength vs. Heat Transport
Strong correlation with thermal conductance
Effectively tune both properties with single monolayer
** Error estimated at ±5% TDTR Measurements appear in Losego et al. Nature Materials, 11, 502-506, (2012)
**
Notes: ----- Meeting Notes (9/26/13 16:41) -----
Discrete bars for the thermal plot

## Slide 16: Back to Interface Strength: AFM Surface Scans
All image scale bars have range of 1.5 nm
FS/MUTMS
Underside of Au
Scan in graph above indicated on green highlighted portion of image
Bare FS
Surface roughness of SAM comparable to SAM thickness

## Slide 17: Surface Roughness: Si vs. Fused Silica
Silicon provides lower roughness (1.2 Å) substrate surface than FS (7.4 Å)
Spallation strength of MUTMS
  on Si: ~ 200 MPa
  on FS: ~ 85 MPa
Si/MUTMS
FS/MUTMS
AFM Scans

## Slide 18: Rigid/Static Separation: 1D Mesoscale Model
Au
2A
SAM
surface
Effective cohesive traction
where
L (>>A)
Same length scale:
SAM thickness
surface roughness
MD cutoff radius

## Slide 19: Rigid/Static Separation: 1D Results
where

## Slide 20: Rigid/Static Separation: 2D Results
For the current system,
Incorporation of surface roughness significantly reduces average cohesive traction

## Slide 21
Deformable Film Model
Chart: 
From MD Simulations
Governing Differential Equation
Boundary Conditions
Notes: 21

## Slide 22
Non-dimensional Equations
Non-dimensional
Parameters
Governing
Differential
Equation
Boundary Conditions
Typical thin film substrate system
Notes: 22

## Slide 23
Initial Profile & Bending Energy
Notes: 23

## Slide 24
Initial Profile & Bending Energy
Notes: 24

## Slide 25
Initial Profile & Bending Energy
Notes: 25

## Slide 26
Bending Energy vs. (β , η)
Notes: 26

## Slide 27
“Rigid Spallation” : spallation process too fast for dynamic bending effect to take place
Spallation: Quasi-Static Model
Notes: 27

## Slide 28
Effective Cohesive Law
Notes: 28

## Slide 29
Effective Cohesive Law
Notes: 29

## Slide 30
Effective Cohesive Law
Notes: 30

## Slide 31
Effect of Roughness on Cohesive Energy
Notes: 31

## Slide 32: Conclusions and Current/Future Work
Interfacial strength of SAM-mediated interfaces strongly dependent on functional group chemistry
MD simulations point to drastic difference in strength and work of separation between methyl and thiol terminated SAMs
Incorporation of surface roughness critical in obtaining effective cohesive properties
Current/Future Work
  MD simulations of correlation between failure and thermal properties
  Dynamic analysis of impact of roughness on failure properties
  Effect of randomness
  ‘3D real surfaces’
  Delamination of SAM-enhanced interfaces

## Slide 33: Thank You
Philippe H. Geubelle
Aerospace Engineering and Beckman Institute
University of Illinois Urbana Champaign
306 Talbot Laboratory 104 S Wright St. Urbana IL 61801
geubelle@illinois.edu
Grady, M. E., Geubelle, P. H., Braun, P. V., and Sottos, N. R. (2014) “Molecular tailoring of interfacial failure.” Langmuir. DOI: 10.1021/la502271k.