## Slide 1
Chen Zhang, Graduate Student
Aerospace Engineering
Nancy R. Sottos, Professor
Materials Science and Engineering
Jaeuk Sung, Graduate Student
Materials Science and Engineering
University of Illinois at Urbana-Champaign, USA
Philippe H. Geubelle, Professor
Aerospace Engineering
Dynamic Spallation of Film/Substrate Interfaces Tailored with Self-Assembled Monolayers:
A Multiscale Model on Interface Roughness Effect

## Slide 2: Self-Assembled Monolayers
Ordered molecular assemblies formed spontaneously on surfaces by adsorption
Each unit comprises of the ‘head group’, ‘tail’ and ‘functional group’
Monolayer kept intact by Van der Waals interactions
Applications
  Wetting and adhesion
  Chemical resistance
  Nano-fabrication
  For studying membrane properties of cells
  Commercial application example: Rain-X
  Bio-compatibility
  Thermal management of nano-electronics
  Surface modifiers of MEMS and NEMS
Scanning tunneling microscope image (15 nm x 15 nm) of a SAM of n-decanethiolate on Au{111} (Paul Weiss’ group, PSU)
SURFACE
MODIFIERS
INTERFACE
TAILORING
~ 1 nm

## Slide 3: Materials
Self-assembling molecules (Gelest inc.)
Chemical | Formula | Shorthand Name
Dodecyltriethoxysilane | CH3(CH2)11Si(OC2H5)3 | DTES
11-mercapto-undecyltrimethoxysilane | SH(CH2)11Si(OC2H5)3 | MUTMS
11-bromo-trimethoxysilane | Br(CH2)11Si(OC2H5)3 | BrUTMS
11-amino-trimethoxysilane | NH2(CH2)11Si(OC2H5)3 | ATES
NH2
Br
SH
CH3
Mixed Monolayers
50% mole percent in solution
SiO2 Substrate
Notes: Also describe mixed monolayers here as well

## Slide 4: Molecular Dynamics Simulations
Silica/SAM/Gold model built using Materials Studio
In-plane periodic unit cell of size 25A x 25A x 40A (Contains about 1500 atoms)
Captures SAM tilt with respect to Silica layer
Thermal equilibrium (at 300K) and spallation simulations performed using LAMMPS
MD analysis based on ReaxFF potential to model bond failure (Jarvi et al., J. Phys. Chem. A, 2011)
“Smooth” application of constant velocity along top Au atomic layers
Dodecyltriethoxysilane | CH3(CH2)11Si(OC2H5)3 | DTES
11-mercapto-undecyltrimethoxysilane | SH(CH2)11Si(OC2H5)3 | MUTMS
Velocity imposed on gold layer
Awasthi et al. Mech. of Mater., 2016

## Slide 5: MD Predicted Cohesive Law
T=300K, V0=30m/s
DTES
MUTMS
Work of separation ~ 0.3 J/m2
Interfacial strength ~ 0.75 GPa
Work of separation ~ 0.6 J/m2
Interfacial strength ~ 3 GPa
Awasthi et al., 2016

## Slide 6: SAM Functionalization Procedure
Piranha Solution
Clean
SAM bath
24 hours
SAM molecule, amine catalyst, toluene
Rinse Toluene, Ethanol,
DI water,
blown dry
Ellipsometry
Transfer Printing
Material Characterization
X-ray Photoelectron Spectroscopy (XPS)
Atomic Force Microscopy (AFM)
SAM layer thickness ~ 1 nm
Surface topography, surface roughness
Chemical information
“Soft” lithography process
Technique
Information Acquired

## Slide 7: Transfer Printing Method
Use PDMS stamp to peel off gold
Transfer Print to New Substrate
Peel off PDMS
SiO2/SAM/Au
2
1
3
4
Deposit Au on donor substrate
Losego et al. Nat. Mater., 2012

## Slide 8: Interfacial Strength Measurement
Specimen Schematic
Laser Spallation Technique
Developed by: Vossen (1976), Gupta (1992)
Wang, Weaver & Sottos (2002)
14 mJ/mm2
16 mJ/mm2
21 mJ/mm2
12 mJ/mm2
Notes: The laser-induced ablation of the confined Al absorbing layer results in the generation of a high amplitude compressive acoustic pulse, with a rise time comparable to that of the impinging light pulse. Upon reaching the free surface of the test film, the compressive pulse reflects back as a tensile pulse and loads the interface of interest in tension. If the magnitude of this tensile stress pulse is greater than the interfacial adhesion strength, the test film spalls from the substrate. 234 nm. 16.5 ns
yttrium aluminum garnet

## Slide 9: Experiments Predicted Interfacial Strength
Interface strength determined at interface stress that initiates film failure in >85% tests
Good: MUTMS/DTES strength ratio similar
Bad: Off by a factor of 30…50
Experimental | Numerical (MD)
25 MPa | 0.75 GPa
85 MPa | 3 GPa
DTES
MUTMS
Interfacial Strength
Grady et al., 2015

## Slide 10: “Side note”: Interface Strength vs. Heat Transport
Strong correlation with thermal conductance
Effectively tune both properties with single monolayer
** Error estimated at ±5% TDTR Measurements (Losego et al., Nature Materials, 11, 502-506, 2012)
**
Notes: ----- Meeting Notes (9/26/13 16:41) -----
Discrete bars for the thermal plot

## Slide 11: Surface Roughness: Si vs. Fused Silica
Measured spallation strength
  Si: ~ 200 MPa
  FS: ~ 85 MPa
Si/MUTMS
FS/MUTMS
AFM Scans
Recall:
Cohesive length scale ~ 0.2 nm
SAM layer thickness ~ 1 nm

## Slide 12
Effect of Surface Roughness: Continuum Model
Contact Region
with
Governing Differential Equation
Periodic BC
Chart: 
Chart: 
From MD Simulations
T
Notes: 12

## Slide 13
Non-Dimensional Equations
Typical thin film substrate system
Notes: 13

## Slide 14
Step1: deformed shape of transfer-printed film
Notes: 14

## Slide 15
Step1: deformed shape of transfer-printed film
Notes: 15

## Slide 16
Step1: deformed shape of transfer-printed film
Notes: 16

## Slide 17
Bending Energy: Wavelength Ratio
Notes: 17

## Slide 18
Step2: Quasi-Static Spallation Model
“Rigid Spallation” : spallation process too fast for dynamic bending effect to take place
Notes: 18

## Slide 19
Effective Cohesive Law Example
Notes: 19

## Slide 20
SAM Real Surface Profile
DTES - Fused Silica
100nm*100nm

## Slide 21
Maximum Effective Traction
Different Values of
Notes: 21

## Slide 23
Surface Bearing Distance
Notes: 23

## Slide 24
Sr Distribution
Notes: 24

## Slide 25
Effect of Sr on Spallation Strength
Notes: 25

## Slide 26
Correlation (and lack thereof…)
Notes: 26

## Slide 27
Correlation vs. Sr(D)
Notes: Self assembly monolayer and Interfacial fracture energy

## Slide 28
Effect of SAM on Dynamic Delamination

## Slide 29: Dynamic Delamination Test
a0
L
Applied stress wave
1-D elasto-dynamic analysis
Interfacial stress vs. kinetic energy
Gc
Notes: Different from the spectral/FE method, the nonlinear beam model simulate the consequent delamination process after the spallation failure of the precrack
At that point, the precrack is lifted off the substrate at certain velocity V0 which can be determined by a simple 1D wave propagation analysis as illustrated below
In this 1D analysis, this average velocity can be determined from the total kinetic energy trapped in the pre-crack region of the film

## Slide 30: Illustration: Al on Si
Tran, Kandula, Geubelle and Sottos, EFM, 2008
Kandula, Hartfield, Geubelle and Sottos, Thin Solid Films, 2008
Kandula, Tran, Geubelle and Sottos, App. Phys. Letters, 2008
Tran, Kandula, Geubelle and Sottos, IJF, 2010
Notes: Here is an example of the deformation of the film using the beam model and for comparison, we have here also the experimental results
We got here 3 micron Al Film with 300 micron precrack which is similar to the adhesion test configuration
It clearly shows that the film experience large deformation and large rotation
The comparison with 2D model is presented in the next slide ……

## Slide 31
Evolution of Kinetic Energy During Pulse Loading

## Slide 32
Delaminated Gold Strip (100% MUTMS)
250 mm

## Slide 33
All scale bars: 250 mm
Effect of SAM on Delamination
M100D0
M75D25
M50D50
M25D75

## Slide 34
Interface Fracture Toughness

## Slide 35: Conclusions
Interfacial strength of SAM-mediated interfaces strongly dependent on functional group chemistry
MD simulations point to drastic difference in strength and work of separation between methyl- and thiol- terminated SAMs
Incorporation of surface roughness critical in obtaining effective cohesive properties
  Idealized surface model
  Real SAM surface model
Single parameter not enough to capture roughness effect for compliant films
Experimental evidence of strong dependence of SAM functional group on interface fracture toughness
M100D0
M75D25
M50D50
M25D75

## Slide 36: Wang, Liechti et al., JAM, 2006
Indentation Punch
SAM + substrate
Force
Disp.
Force
Disp.
Force
Disp.
Force
Disp.
OTS-Tungsten system

## Slide 37
Figure 4. Calibration data (a) Average peak substrate stress versus fluence, and (b) Average peak interface stress versus laser fluence.

## Slide 39
Figure 5. Optical images of film failure caused by laser induced stress wave to DTES interface(weak adhesion layer) at increasing stress amplitude. Scale bar is 500 mm

## Slide 40
Max Effective Traction, Rigid Film
Notes: 40

## Slide 41
Captured Variance Using Sr(D)
Notes: Self assembly monolayer and Interfacial fracture energy

## Slide 42
Bare FS
All image scale bars have range of 1.5 nm
FS/MUTMS
Underside of Au
Scan in graph above indicated on green highlighted portion of image
Recall:
Cohesive landscape ~ 0.2 nm
SAM layer thickness ~ 1 nm
Martha Grady et al.

## Slide 43
Maximum Effective Traction
Change of by
Patch size
Notes: 43

## Slide 44
SAMs Surface Profile: MUTMS 1

## Slide 45
SAM Real Surface Profile
DTES - Fused Silica
100nm*100nm

## Slide 46
SAMs Surface Profile: MUTMS 2

## Slide 47
Surface Bearing Distance
Notes: 47